ANNEX 2

to the Contract No._____ of _________ 2024

TENDER

Part 2 of the Procurement.

Headover

TECHNICAL CHARACTERISTICS OF THE HEADOVER KNITTED FABRIC

| No. | Name of the parameter, dimension | Indicator value | Indicator value (specify)** |
| --- | --- | --- | --- |
| 1. | Composition of raw material, | 95±2 % PES 5±2 % EL | 93,4% PES 6.6 EL |
| 2. | Surface density, g/m2 | 150,0 +20,0; -10,0 | 156 |
| 3. | Dimensional variation after washing and drying (lateral and longitudinal directions ), % (*) | 2,0 | -1,3 longitudinal - 1,7 lateral |
| 4. 4.1. 4.2. 4.3. | Paint resistance, points - for washing at 40 °C (*) - for sweat - for dry abrasion | ≥ 4 ≥ 4 ≥ 4 | 4-5 4-5 4-5 |
| 5. | Wear resistance, pumps | 50 000 | 50 000 |
| 6. | Pumping (after 30 min), degree | ≥ 4 | 4-5 |

- **The Supplier must fill in the column “Indicator value”, indicating the specific value of each technical indicator to which the proposed goods conform (technical indicators whose conformity is certified by test reports from a laboratory accredited according to international standards shall be extracted from the report)