ANNEX 2

to the Contract No._____ of _________ 2024

TENDER

Part 5 of the Procurement.

A SHIRT OF THE TACTICAL FIELD UNIFORM SUIT

TECHNICAL CHARACTERISTICS OF KNITTED FABRIC FOR SHIRTS

| Seq. No. | Name of indicator, dimension |  | Indicator value |  | Indicator value (specify) |
| --- | --- | --- | --- | --- | --- |
| 1. | Fibre composition, % |  | 100 % Polyester |  | 100% Polyester |
| 2. | Surface density g/m2 |  | 220,0 + 20,0/ -10,0 |  | 214 g/m2 |
| 3. | Dimensional variation after washing and drying (transverse and longitudinal directions), % |  | Not more than 5,0 |  | transverse direction – 0 longitudinal direction – +0,5 |
| 4. | Paint resistance, scores |  |  |  |  |
| 4.1. | - for dry abrasion |  | 4 |  | 4 |
| 4.2. | - for wet abrasion |  | 3 |  | 4 |
| 4.3. 4.4. | - for washing at 40oC - for sweat |  | 4 4 |  | 4 4 |
| 5. | Tendency to fluff and lint (after 2 000 revolutions), degree |  | 4 |  | Face side: Pilling after 2000 rubs -5 Fuzzing after 2000 rubs-5 Back side: Pilling after 2000 rubs-5 Fuzzing after 2000 rubs-5 |
| 6. | Wear resistance, 9kPa, pumps |  | ≥ |  | >30 000 |
| 7. | Colour differences, Δ ECMC |  | 1,5 |  | - |

TECHNICAL CHARACTERISTICS OF TEXTILE VELCRO FASTENERS

| Seq. No. | Indicator | Measuring units | Characteristics | Indicator value (specify)) |
| --- | --- | --- | --- | --- |
| 1. | Surface density soft side (loops) coarse (hooks) | g/m 2 | 340±10 320±10 | 350 330 |
| 2. | Dimensional change after washing and drying | % | ≤ 2 | 1 |
| 3. | Colour resistance to washing (discolouration and repainting of material) | scores | ≥ 4 | 4 |
| 4. | Resistance to staining for dry abrasion for wet abrasion | scores | ≥ 4 ≥ 3 | 4 4 |
| 5. | Shear force: Original after 5000 open-close cycles | N/cm | ≥ 8 ≥ 4 | 12,36 11,77 |
| 6. | Separating force: Original after 5000 open-close cycles | N/cm | ≥ 1,3 ≥ 0,65 | 2.01 1.93 |

TECHNICAL CHARACTERISTICS OF ZIPPERS

| Seq. No. | Name of indicator, dimension | Indicator value | Indicator value (specify) |
| --- | --- | --- | --- |
| 1. | Lock pendant breaking strength, N | 250 | 400 |
| 2. | Top braking force, N | 110 | 210 |
| 3. | Number of clasp-unclasp (open-close) cycles without failure, cycles | 500 | 1100 |
| 4. | transverse strength of the tooth track, N | 370 | 850 |
| 5. | locking strength of the lock, N | 40 | 90 |
| 6. | dimensional change after washing*, % | ≤ ± 2 | ≤ ± 1,5 |
| 7. | Paint resistance, points |  |  |
| 7.1. | for artificial light | 5 | 5 |
| 7.2. | for washing* | 4 | 4 |
| 7.3. | for dry abrasion | 4 | 4 |
| 7.4. | for wet abrasion | 3 | 3-4 |