# ANNEX 1

# to the Contract No. DPS- _______ dated                       2024

TECHNICAL SPECIFICATION FOR OUTDOOR BOOTS - General requirements - Outdoor boots (hereinafter referred to as outdoor boots) - designed to be worn by soldiers of all branches of the armed forces during the warm season at ambient temperatures between +6º C and +30º C. - Outdoor boots are designed to protect soldiers’ feet from physical injury and trauma, as well as to ensure the comfort and stability of the foot during military field exercises or everyday service tasks. - Outdoor boots shall be certified in accordance with EN/ISO 20347 or equivalent and shall comply with the requirements set out in this Technical Specification. - Outdoor boots shall be brown leather lace-up boots with a lining (without membrane), a continuous patterned sole and a rubber protective rim (the PANTONE colour codes for the individual materials are given in Table 2 “Requirements for basic materials (technical characteristics)” of the technical specification, hereinafter referred to as Table 2). - The quality of the boots shall be guaranteed for a minimum period of 12 months of active use, starting from the date of issue of the Goods from the Buyer’s warehouse, and 24 months from the date of signature of the documents of acceptance of the Goods into the warehouse. - Technical requirements - All measurements and values are for a basic 270 shoe size. - The weight of a pair of outdoor boots (size 270) must be ≤ 1,6 kg. - The height of the bootleg of outdoor boots, measured from the heel part of the insole to the highest part of the bootleg (excluding the tongue), must be 17,5 cm ± 1,0 cm (for size 270, as determined in accordance with EN ISO 20344, p. 6.2, or an equivalent standard). - The upper of the outdoor boots shall be made of natural waterproof leather (breathable hydrophobic nubuck leather) (the colour and technical characteristics of the upper leather are shown in Table 2 of the technical specification). - The lining shall be a sweat-absorbent, fast-drying, multi-layer laminated material with a soft, abrasion- and wear-resistant feel (see Table 2 of the Technical Specification for the technical characteristics of the lining). - The tongue of the boot shall be anatomically shaped to protect the foot from the effects of shoelaces and eyelets, and shall incorporate padding inside the tongue to ensure comfort, convenience and stability of the instep of the foot (the technical characteristics of the shoe tongue are given in Table 2 of the technical specification). - The tongue of the shoe shall be made of leather in such a way that it does not physiologically reduce or impair the flexibility of the shoe at the instep. The tongue must include a feature (eyelet or other solution) to secure the tongue of the shoe to the laces. - To protect the foot from moisture, sand, pebbles or other unwanted agents entering the inside of the shoe, the tongue of the shoe must be connected to the sides of the shoe by additional leather fittings. - Outdoor boots must support the foot at the ankle and keep it stable when walking, running, crawling, squatting, etc. The bootleg of the boot must anchor the ankle and limit the lateral rotational movement of the foot. - The outer sole shall have a tactile surface (roughened), a coarse pattern, be anti-static, resistant to oil, hydrolysis and wear, and be made of a composite of rubber and PU or a composite of rubber and micro rubber. The pattern shall be designed so that the pointed protrusions of the pattern are oriented in different directions in relation to the ground resistance and grip the moving surface or support. The technical characteristics of the sole are given in Table 2 of the technical specification (PU midsole colour close to Pantone 19-0910 TPX). - The toe and heel of the shoe shall be covered externally at the junction with the sole with an additional protective rubber detail (tape) to better repel dirt and to protect the shoe from mechanical damage. The front rubber toe guard shall measure 30 ± 5 mm from the upper lip of the sole, with a length of 150 ± 10 mm with a slope towards the sole. Rubber heel protector measured from the upper lip of the heel 45 ± 5 mm, length 120 ± 10 mm with a slope to the sole for size 270 (other design solutions are possible). The colour of the rubber heel protector shall be similar to Pantone 19-0910 TPX. - The upper part of the bootleg (soft cantle) shall be padded and shall have ventilation openings to ensure air circulation. The diameter of the ventilation holes shall be 3 mm - 4 mm. - The upper part of the sides of the upper, where the ankle bones are in contact with the ankle, must be protected by outer parts made of thermoplastic PU (or equivalent) (colour similar to Pantone 19-1015 TPX) and the inner side must be padded with a foam that adapts to the body’s shape. - The toe section of the boot must protect the toe area from external influences and ensure that the front of the boot is resistant to deformation and must therefore be made of thermoplastic/polyester or its equivalent. The technical characteristics of the toe cap are set out in Table 2 of the technical specification. - The heel of the shoe must be secured by the back of the shoe. The solid heel shall conform to the shape of the heel of the foot, maintain stability of the heel (the heel shall not roll in the shoe) and be moulded in thermoplastic or equivalent material. The inner part of the heel shall be made of 2 to 3 mm thick cellulose/fibrous leather or equivalent material. - Outdoor boots must be made with anti-static properties. Anti-static properties shall be provided by anti-static tape or other equivalent construction inside the boot. - Outdoor boots must be able to accommodate the individual corrective foot inserts required for a stumpy foot. - Outdoor boots shall have insoles that absorb the impact of walking, reduce friction on the sole of the foot, absorb perspiration and keep the foot in the correct position, and be replaceable and washable at 30°C. The insoles shall conform to the geometry of the plantar surface of the foot, the technical characteristics of which are given in Table 2 of the technical specification. - Insole: two layers, made of PU foam, with a top layer made of microfibre or equivalent material. - Insole (winter): two layers, made of PU foam, the top layer made of polyester non-woven or equivalent material. - The shoe shall have a quick lacing system consisting of low friction metal eyelets, fastening rings and a quick lock. - A stretchable pocket shall be provided in the outer part of the upper or in the tongue to accommodate the ends of the laces. A fastening loop at the back of the shoe made of a textile strip. - The static compliance of the shoe must be ensured in the manufacture of the shoe (the foot to shoe ratio, where the shoe fits snugly against the foot, is neither too high nor too low). - The shoes shall be manufactured in a range of at least size 35 to 51 in accordance with ISO 9407 or, as appropriate, size 225 to 330 in 3 different fullnesses (as indicated in Table 1). # SIZES # Table 1 Boot size; Boot size equivalent; Boot width 1; Boot width 1; Boot width 1. Foot length, mm; Size according to the system; Foot circumference, mm; Foot circumference, mm; Foot circumference, mm. 225; 35; 232; 238; 245. 230; 36; 234,5; 240,5; 247,5. 235; 37; 237; 243; 250. 240; 37,5; 239,5; 245,5; 252,5. 245; 38; 242; 248; 255. 250; 39; 248; 254; 261. 255; 40; 251; 257; 264. 260; 41; 253,5; 259,5; 266,5. 265; 41,5; 256,5; 262,5; 269,5. 270; 42; 259; 265; 272. 275; 43; 264; 270; 277. 280; 44; 267; 273; 280. 285; 45; 269,5; 275,5; 282,5. 290; 45,5; 272; 278; 285. 295; 46; 274,5; 280,5; 287,5. 300; 47; 280; 286; 293. 305; 48; 285,5; 291,5; 298,5. 310; 49; 288; 294; 301. 320; 50; 293; 299; 306. 330; 51; 295,5; 301,5; 308,5. REQUIREMENTS FOR BASIC MATERIALS (TECHNICAL CHARACTERISTICS) Table 2 No.; Parameter name; Dimension; Parameter value; Test method identifier. General footwear requirements. 1.; Resistance to contact with hot surfaces; symbol HRO; EN ISO 20344, clause 8.7 or equivalent. 2.; Water resistance; symbol WR; EN ISO 20344 clause 5.15.2 or equivalent. 3.; Slip resistance; symbol SRC; EN ISO 20344 clause 5.11 or equivalent. 4.; Fuel and oil resistance; ≤ 2,5 %; symbol FO; EN ISO 20344 clause 8.6 or equivalent. 5.; Thermal insulation (temperature change); ˚C; symbol HI ≤ 14,0; EN ISO 20344 clause 5.12 or equivalent. 6.; Cold insulation (temperature change); ˚C; symbol CI ≤ 10,0; EN ISO 20344 clause 5.13 or equivalent. 7.; Energy absorption in the heel area; J; ≥ 30; EN ISO 20344 clause 5.14 or equivalent. 8.; Ankle protection; symbol AN; EN ISO 20344 clause 5.14 or equivalent. Requirements for the upper layer (colour close to Pantone 18-1027 TPX). 11.; Thickness; mm; 2,0 – 2,2; EN ISO 2589 or equivalent. 12.; Tear load (double edge); N; ≥ 300; EN ISO 20344 clause 6.3 or equivalent. 13.; Water penetration time; min; ≥ 360; EN ISO 20344 clause 6.13 or equivalent. 14.; Water vapour transmission; mg/cm2h; ≥ 7,0; EN ISO 20344 clause 6.6, EN ISO 14268 or equivalent. Requirements for tongue, upper part of the bootleg and heel layer (colour close to Pantone 19-1218 TPX). 15.; Thickness; mm; 1,1 – 1,3; EN ISO 2589 or equivalent. 16.; Resistance to folding, without fibre cracking dry wet; cycles; ≥ 100 000 ≥ 50 000; EN ISO 5402-1 or equivalent. 17.; Water vapour transmission; mg/cm2h; ≥ 9,0; EN ISO 20344 clause 6.6, EN ISO 14268 or equivalent. 18.; Water penetration time; min; ≥ 360; EN ISO 20344 clause 6.13, EN ISO 5403-1 or equivalent. 19.; Tear load (double edge); N; ≥ 100; EN ISO 20344 clause 6.3 or equivalent. Lining. 20.; Thickness; mm; 1,3 ± 0,1; specify. 21.; Basic weight; g/m²; ≤ 360; specify. 22.; Tearing force; N; ≥ 80; EN ISO 20344 clause 6.3 or equivalent. 23.; Water vapour transmission; mg/cm²h; ≥ 30; EN ISO 20344 clause 6.6, EN ISO 14268 or equivalent. 24.; Abrasion resistance dry wet; cycles; ≥ 400 000 ≥ 200 000; EN ISO 20344 clause 6.12, EN ISO 12947-2 Or equivalent. Tongue lining, lining of the upper part of the bootleg. 25.; Knitted polyster fabric; g/m²; ≤ 210. 26.; Tearing force; N; ≥ 17; EN ISO 20344 clause 6.3 or equivalent. 27.; Water vapour transmission; mg/cm²h; ≥ 50; EN ISO 20344 clause 6.6, EN ISO 14268 or equivalent. 28.; Abrasion resistance dry wet; cycles; ≥ 100 000 ≥ 50 000; EN ISO 20344 clause 6.12 or equivalent. Inner heel material. 29.; Thickness; mm; 1,1-1,3; EN ISO 2589 or equivalent. 30.; Tearing force; N; ≥ 30; EN ISO 20344 clause 6.3 or equivalent. 31.; Water vapour transmission; mg/cm²h; ≥ 10; EN ISO 20344 clause 6.6, EN ISO 14268 or equivalent. 32.; Abrasion resistance dry wet; cycles; ≥ 500 000 ≥ 170 000; EN ISO 20344 clause 6.12, EN ISO 12947-2 , or equivalent. Removable insole. 33.; Water absorption; mg/cm²; ≥ 220; EN ISO 20344 clause 7.2 or equivalent. 34.; Water desorption; %; ≥ 99; EN ISO 20344 clause 7.2 or equivalent. 35.; Abrasion resistance dry wet; cycles; ≥ 200 000 ≥ 100 000; EN ISO 20344 clause 6.12, EN ISO 12947-2 , or equivalent. Hot climate insole (perforated). 36.; Water absorption; mg/cm²; ≥ 200; EN ISO 20344 clause 7.2 or equivalent. 37.; Water desorption; %; ≥ 99; EN ISO 20344 clause 7.2 or equivalent. 38.; Abrasion resistance dry wet; cycles; ≥ 350 000 ≥ 80 000; EN ISO 20344 clause 6.12, EN ISO 12947-2 , or equivalent. Toe cap part (thermoplastic/polyester or equivalent material). 39.; Thickness; mm; 1,1 – 1,3; specify. 40.; Weight; g/m²; 1000 – 1100; specify. Sole (rubber sole) (close to Pantone 19-1101 TPX). 41.; Protector depth; mm; ≥ 5,0; EN ISO 20344 clause 8.1.2 or equivalent. 42.; Tearing force; kN/m; ≥ 20; EN ISO 20344 clause 8.2 or equivalent. 43.; Abrasion resistance; mm³; ≤ 120; EN ISO 20344 clause 8.3 or equivalent.

- Labelling, packaging and acceptance

  - Once the Contract is concluded, working samples are agreed and approved as a basis for acceptance of the products.

  - For the acceptance of the working sample, the Supplier shall provide:

- Two identical products;

- instructions for use/maintenance for coordination, which must describe the product’s features, purpose, and provide information on how to put on, wear and maintain the shoes correctly) (the instructions will have to be attached to each pair of shoes, or can be provided by a QR code on the shoe label;

- a technical description of the product, together with documents (test reports, certificates, manufacturer’s approvals, etc.) attesting that the materials (leather, hardware, etc.) used in the manufacture of the product comply with the requirements set out in the technical specification.

  - Mass production is only permitted after approval of working samples.

  - Footwear shall be marked with a label on the tongue of the shoe, on the inside of the bootleg, or in a prominent position indicating:

- size (the sizing shall be coordinated at the time of alignment of the working sample);

- manufacturer’s name or trademark;

- Contract date and number;

- batch and consignment index;

- date of manufacture.

  - The label must be reliable and the labelling particulars must be of sufficient size to allow easy reading of the information provided.

  - Footwear shall be packed in pairs in boxes. Boxes shall be resistant to long storage and multiple transport with ventilation holes (minimum 3). Each box shall contain a care instruction and be labelled with a label stating:

- supplier’s name or trademark;

- manufacturer’s name or trademark (if different from the supplier);

- for imported goods, the country of origin of the goods, if this is not the same as the country in which the manufacturer’s registered office is situated;

- product name;

- size (the sizing shall be coordinated at the time of alignment of the working sample);

- Contract date and number;

- batch and consignment index;

- date of manufacture.

  - The boxes are placed in cardboard boxes. Boxes shall be resistant to long storage and multiple transport. Each box shall contain only one size of footwear. The cardboard boxes shall be labelled with the following information:

- supplier’s name and trademark;

- manufacturer’s name or trademark (if different from the supplier);

- for imported goods, the country of origin of the goods, if this is not the same as the country in which the manufacturer’s registered office is situated;

- product name;

- size;

- quantity;

- Contract date and number;

- batch and consignment index;

- Date of manufacture.

  - Product packaging shall comply with the minimum environmental criteria set out in Annex 2 of the Procedure Description for the Application of Environmental Criteria in Green Procurement, approved by the Order of the Minister of the Environment of the Republic of Lithuania No. D1-401 of 13 December 2022 “Regarding the Order of the Minister of the Environment of the Republic of Lithuania of 28 June 2011 No. D1-508 “On the approval of the list of products for which environmental criteria are applicable to public procurement and purchasing, the list of environmental criteria and the description of the procedure for the application of environmental criteria to be applied by contracting authorities and contracting entities when purchasing goods, services or works”, section II “Packaging”.

  - Products are accepted in batches and consignments. Each batch of goods shall be marked with a contractual mark and shall be accompanied by a declaration of conformity by the manufacturer of the goods in accordance with LST EN ISO/IEC 17050-1(ISO/IEC 17050-1) Form A.2 or equivalent and by documents proving the conformity of the materials with the technical characteristics of the requirements.

  - Footwear shall be accepted on the basis of an approved working sample. Both pairs of boots must be of the same size, pattern and material, and the materials used to make the boots must not differ between the pairs. The Buyer shall check the quality of the goods at random from the selected batch and may carry out laboratory tests in accordance with the terms of the contract. In the event that the results of the tests do not meet the technical requirements, the entire batch shall be subject to defects.