ANNEX 2

to the Contract No._____ of _________ 2024

TENDER

TECHNICAL CHARACTERISTICS

| No. | Parameter name Dimension | Indicator value (specify) |
| --- | --- | --- |
| 1 | The height of the bootleg of outdoor boots, measured from the heel part of the insole to the highest part of the bootleg (excluding the tongue), must be 17,5 cm ± 1,0 cm (for size 270, as determined in accordance with EN ISO 20344, p. 6.2, or an equivalent standard). | 17,5 cm |
| 2 | The weight of a pair of outdoor boots (size 270) must be ≤ 1,6 kg | 1,558 kg |
| 3 | The quality of the boots shall be guaranteed for a minimum period of 12 months of active use, starting from the date of issue of the Goods from the Buyer’s warehouse | 12 months |
| 4 | The quality of the shoes is guaranteed for at least 24 months from the date of signing the goods acceptance documents. Goods in stock. | yes |
|  | General footwear requirements |  |  |
| 5. | Resistance to contact with hot surfaces, symbol HRO | yes |
| 6. | Water resistance, symbol WR | yes |
| 7. | Slip resistance, symbol SRC | yes |
| 8. | Fuel and oil resistance, symbol FO, ≤ 2,5 % | ≤ 1,0 % |
| 9. | Thermal insulation (temperature change) symbol HI, ≤ 14,0 ˚C | ≤ 11,9 ˚C |
| 10 | Cold insulation (temperature change) symbol CI, ≤ 10,0 ˚C | ≤ 4,3 ˚C |
| 11. | Energy absorption in the heel area ≥ 30 J | ≥ 31,5 J |
| 12. | Ankle protection, symbol AN | yes |
|  | Requirements for the upper layer (colour close to Pantone 18-1027 TPX) |  |  |
| 13. | Colour close to Pantone 18-1027 TPX | yes |
| 14. | Thickness, 2,0 – 2,2mm | 2,12 mm |
| 15. | Tear load (double edge) ≥ 300N | ≥ 329 N |
| 16. | Water penetration time ≥ 360 min | ≥ 480 min |
| 17. | Water vapour transmission ≥ 7,0 mg/cm2h | ≥ 9,22 mg/cm2h |
|  | Requirements for tongue, upper part of the bootleg and heel layer (colour close to Pantone 19-1218 TPX) |  |  |
| 18. | Colour close to Pantone 19-1218 TPX | yes |
| 19. | Thickness, 1,1 – 1,3 mm | 1,27 mm |
| 20. | Resistance to folding, without fibre cracking dry≥ 100 000 wet≥ 50 000 cycles | ≥ 100 000 ≥ 50 000 |
| 21. | Water vapour transmission ≥ 9,0 mg/cm2h | ≥ 9,1 mg/cm2h |
| 22. | Water penetration time ≥ 360 min | ≥ 360 min |
| 23. | Tear load (double edge) ≥ 100N | ≥ 108,4 N |
|  | Lining |  |  |
| 24. | Thickness, 1,3 ± 0,1 mm | 1,29 mm |
| 25. | Basic weight ≤ 360 g/m² | ≤ 348 g/m² |
| 26. | Tearing force ≥ 80N | ≥ 126 N |
| 27. | Water vapour transmission ≥ 30 mg/cm²h | ≥ 49,19 mg/cm²h |
| 28. | Abrasion resistance dry≥ 400 000 cycles wet≥ 200 000 cycles | ≥ 400 000 ≥ 200 000 |
|  | Tongue lining, lining of the upper part of the bootleg |  |  |
| 29. | Knitted polyster fabric ≤ 210 g/m² | 200 g/m² |
| 30. | Tearing force ≥ 17 N | ≥ 19,5 N |
| 31. | Water vapour transmission ≥ 50 mg/cm²h | ≥ 62,70 mg/cm²h |
| 32. | Abrasion resistance dry≥ 100 000 cycles wet≥ 50 000 cycles | ≥ 200 000 ≥ 100 000 |
|  | Inner heel material |  |  |
| 33. | Thickness1,1-1,3 mm | 1,24 mm |
| 34. | Tearing force ≥ 30N | 32 N |
| 35. | Water vapour transmission ≥ 10 mg/cm²h | 12,7 mg/cm²h |
| 36. | Abrasion resistance Dry ≥ 500 000 cycles Wet ≥ 170 000 cycles | ≥ 1 250 000 ≥ 170 000 |
|  | Removable insole |  |  |
| 37. | Water absorption ≥ 220 mg/cm² | ≥ 240,6 mg/cm² |
| 38. | Water desorption ≥ 99 % | 100% |
| 39. | Abrasion resistance dry≥ 200 000 cycles wet≥ 100 000 cycles | ≥ 470 000 ≥ 150 000 |
|  | Hot climate insole (perforated) |  |  |
| 40. | Water absorption ≥ 200 mg/cm² | ≥ 225,2 mg/cm² |
| 41. | Water desorption ≥ 99% | 100% |
| 42. | Abrasion resistance dry≥ 350 000 cycles wet≥ 80 000 cycles | ≥ 400 000 ≥ 85 000 |
|  | Toe cap part (thermoplastic/polyester or equivalent material) |  |  |
| 43. | Thickness1,1 – 1,3 mm | 1,22 mm |
| 44. | Weight 1000 – 1100 g/m² | 1078,5 g/m² |
|  | Sole (rubber sole) (close to Pantone 19-1101 TPX) |  |  |
| 45. | Close to Pantone 19-1101 TPX | yes |
| 46. | Protector depth ≥ 5,0 mm | 5,5 mm |
| 47. | Tearing force ≥ 20 kN/m | ≥ 36,40 kN/m |
| 48. | Abrasion resistance ≤ 120 mm³ | ≤ 90,38 mm³ |