ANNEX 2

to the Contract No._____ of _________ 2025

TENDER

TECHNICAL CHARACTERISTICS

| No. | Required technical characteristics of the goods | Specific values for the product indicators offered by the supplier** |
| --- | --- | --- |
| 1 | The height of the instep of the outdoor boot, measured from the heel part of the insole to the highest part of the instep (without the tongue), must be 18,5 cm ± 1,0 cm (for size 270, as determined in accordance with EN ISO 20344 , page 6.2 or equivalent). | 18,7 cm |
| 2 | The weight of a pair of outdoor shoes (size 270) shall be ≤ 1,7 kg | 0,779 kg per boot |
| 3 | The quality of the shoes shall be guaranteed for a period of not less than 12 months under conditions of active use starting from the date of issue of the goods from the Buyer’s warehouse | 12 months |
| 4 | The quality of the shoes shall be guaranteed for a period of not less than 24 months from the date of signing of the documents of acceptance of the goods into the warehouse | Yes |
|  | General requirements for footwear |  |
| 5 | Resistance to contact with hot surfaces, simbol HRO | Yes |
| 6 | Water resistance, simbol WR, ≥ 500.000 cycles | 500.000 cycles |
| 7 | Slip resistance, simbol SRC | Yes |
| 8 | Resistance to fuels and oils, simbol FO, ≤ 2,5 % | 1,0% |
| 9 | Thermal insulation (temperature increases) simbol HI, ≤ 18,0 ˚C | 11,9 ˚C |
| 10 | Cold insulation (temperature reduction), simbol CI, ≤ 7,5 ˚C | 4,3 ˚C |
| 11 | Energy absorption in the heel area ≥ 30 Joule | 32 J |
| 12 | Ankle protection, simbol AN | Yes |
|  | Leather requirements (close to Pantone 18-1027 TPX) |  |
| 13 | The color is close to Pantone 18-1027 TPX | Yes |
| 14 | Thickness 2,0 – 2,2 mm | 2,12 mm |
| 15 | Tearing load (double edge) ≥ 300 N | 329 N |
| 16 | Water penetration time ≥ 360 min | 480 min |
| 17 | Water vapour transmission ≥ 7,0 mg/cm2h | 9,22 mg/cm2h |
|  | Requirements for the tongue, upper bootleg and heel (close to Pantone 19-1118 TPX) |  |
| 18 | The color is close to Pantone 19-1118 TPX | Yes |
| 19 | Thickness 1,1 – 1,3 mm | 1,12 mm |
| 20 | Resistance to folding, without fibre breakage, cycles: dry ≥ 100.000 wet≥ 50.000 | dry 100.000 wet 100.000 |
| 21 | Water vapour transmission, ≥ 7,0 mg/cm2h | 7,37 mg/cm2h |
| 22 | Water penetration time, ≥120 min | 120 min |
| 23 | Tearing load (double edge) , ≥80 N | 99 N |
|  | Knitted polyamide fabric (close to Pantone 19-1012 TPX) |  |
| 24 | The color is close to Pantone 19-1012 TPX | Yes |
| 25 | Surface density, ≤ 790 g/m² | 695 g/m² |
| 26 | Tearing force, ≥ 160 N | 211 N |
| 27 | Water vapour transmission, ≥ 30 mg/cm²h | 34,5 mg/cm²h |
| 28 | Water penetration time, ≥ 180 min | 480 min |
| 29 | Abrasion resistance cycles: dry ≥ 200.000 wet ≥ 100.000 | dry 200.000 wet 100.000 |
|  | Tongue (close to Pantone 19-1012 TPX) |  |
| 30 | The color is close to Pantone 19-1012 TPX | Yes |
| 31 | Knitted polyamide fabric, ≤ 450 g/m² | 405,7 g/m² |
| 32 | Tearing force, ≥ 110 N | 116 N |
| 33 | Water vapour transmission, ≥ 50 mg/cm²h | 53,4 mg/cm²h |
| 34 | Water penetration time, ≥ 180 min | 240 min |
| 35 | Abrasion resistance cycles: dry ≥ 200.000 wet ≥ 100.000 | dry 200.000 wet 100.000 |
|  | Tongue lining, lining of the upper part of the bootleg |  |
| 36 | Knitted polyester fabric, ≤ 210 g/m² | 200 g/m² |
| 37 | Tearing force, ≥ 17 N | 19,5 N |
| 38 | Water vapour transmission, ≥ 50 mg/cm²h | 62,7 mg/cm²h |
| 39 | Abrasion resistance cycles: dry ≥ 100.000 wet ≥ 50.000 | dry 200.000 wet 100.000 |
|  | Lining |  |
| 40 | Layer 1 warp knitting composition 70% ± 5% PA 30% ± 5% PES | 71,9% PA 28,1% PES |
| 41 | Layer 2 A two-component membrane composed of (PTFE) | Yes |
| 41 | Layer 3 lining material, 100% PA | Yes |
| 43 | Thickness, 0,7 ± 0,2 mm | 0,68 mm |
| 44 | Abrasion resistance, cycles: dry ≥ 100.000 wet ≥ 50.000 | dry 200.000 wet 50.000 |
| 45 | Abrasion resistance cycles: wet ≥ 50.000 | wet 50.000 |
| 46 | Sweat resistance, ≥ 3 – 4 | 4-5 |
| 47 | Rubbing resistance, ≥ 3 – 4 | 5 |
| 48 | Thermal insulation Rct, ≤ 10,0 (10-³m²K/W) | 8,9 10-³m²K/W |
| 49 | Water vapour transmission Ret, ≤ 8,0 (m²Pa/W) | 6,38 m²Pa/W |
| 55 | Resistance to water penetration, ≥ 2.000 mbar | 2.000 mbar |
| 51 | Water vapour transmission, ≥ 10 mg/cm²h | 11,4 mg/cm²h |
| 52 | Resistance to water penetration at seam intersections, 1 bar | Yes |
| 53 | Resistance to chemical substances, P = 0, R ≥ 95 Penetration index P in % Deviation index R in % Sodium hydroxide 40%, Nitric acid 65% Hydrochloric acid 32% Sulphuric acid 24% | P: 0% R: 95% |
| 54 | Resistance to liquid penetration (No penetration) (AFFF 3%, Sulphuric acid 37%, Sodium hydroxide 30%, Diesel) | Yes |
| 55 | Water tightness after contamination, ≥ 1.000 mbar (AFFF 3%, Sulphuric acid 37%, Sodium hydroxide 30%, Diesel) | 1.000 mbar |
|  | Non-woven inner heel material |  |
| 56 | Thickness, 1,1-1,3 mm | 1,26 mm |
| 57 | Tearing force, ≥ 40 N | 99,7 N |
| 58 | Water vapour transmission, ≥ 10 mg/cm²h | 10,5 mg/cm²h |
| 59 | Abrasion resistance cycles: dry ≥ 500.000 wet ≥ 170.000 | dry 1.500.000 wet 250.000 |
|  | Insert |  |
| 60 | Water absorption, ≥ 220 mg/cm² | 240,6 mg/cm² |
| 61 | Water desorption, ≥ 99 % | 100% |
| 62 | Abrasion resistance cycles: dry ≥ 200.000 wet ≥ 100.000 | dry 470.000 wet 150.000 |
|  | Insert (Winter) |  |
| 63 | Water absorption, ≥ 250 mg/cm² | 277 mg/cm² |
| 64 | Water desorption, ≥ 95 % | 95 % |
| 65 | Abrasion resistance, cycles ≥ 25.600 ≥ 12.800 | dry 25.600 wet 12.800 |
|  | Insole |  |
| 66 | Thickness, 4,5 – 5,5 mm | 5,0 mm |
| 67 | Water absorption, ≥ 70 mg/cm² | 73 mg/cm² |
| 68 | Water desorption, ≥ 99 % | 100 % |
|  | Part of the toecap (thermoplastic, adhesive on one side) |  |
| 69 | Thickness, 1,10-1,20 mm | 1,20 mm |
| 70 | Weight, 1000 – 1050 g/m² | 1040 g/m² |
|  | Padas (Rubber outsole) (Pantone 19-1101 TPX) |  |
| 71 | The color is close to Pantone 19-1101 TPX | Yes |
| 72 | Tread depth ≥ 5,0 mm | 5,5 mm |
| 73 | Tearing force ≥ 20 kN/m | 36,4 kN/m |
| 74 | Abrasion resistance ≤ 120 mm³ | 90,38 mm³ |

| BUYER Defence Materiel Agency under the Ministry of National Defence Acting Director Deputy director Aistė Garunkštytė ____________________________ (signature) L.S. | SELLER HAIX ® Schuhe Produktions – und Vertriebs GmbH Managing Director Stefan Amberger _____________________________ (signature) L.S. |
| --- | --- |